## Slide 1: Cavities for electron spin resonance: predicting the resonant frequency
APS March Meeting, Mar 17, 2016
John S. Colton
Physics Department
Brigham Young University
Co-authors: Kyle Miller
Dr. Ross Spencer
Michael Meehan
Download the code at
http://www.physics.byu.edu/research/coltonlab/cavityresonance
Paper under review by IEEE Transactions
on Microwave Theory and Techniques

## Slide 2: Motivation
Electron spin resonance in semiconductors

## Slide 3: Cylindrical TE011 Resonant Cavity
“011” specifies Bz
  0: no f dependence
  1: one antinode across center
  1: one antinode top to bottom
Strong B field in center by sample
Weak E field in center near sample
  Avoids sample heating & cavity losses
Can modify resonant frequency with dielectric material, e.g. “dielectric resonators”

## Slide 4: About 7-8 years ago…
(a)
Colton et al., Rev Sci Inst, 2009

## Slide 5: What we want…
Design a cavity for desired frequency & mode
 Easily calculate frequency of given design
  And not have to pay ~$2000/year for a commercial software package (CST Microwave Studio or others)
  And have it be more accurate/easier to use than methods we found in literature

## Slide 6: What has previously been done
Requires simple geometries/approximations:
  effective dielectric constants
  lumped circuit model
  coupled mode theory
  mode matching of DRs
  magnetic wall waveguide model
  dielectric waveguide model
More sophisticated solution of wave equation (expensive and/or time consuming):
  finite integration
  finite element analysis
  method of moments

## Slide 7: Our idea:
Expand actual field in terms of the modes of an empty cavity, solve for “Fourier coefficients”
To get the B-field, can use Faraday’s Law:
…or do an expansion in empty cavity Bnmpl modes

## Slide 8
new index
TE Modes
=0
TM Modes
=1
Summation
If cylindrically symmetric: fix m
If m = 0: fix l

## Slide 9: One page of math
Use a vector identity, substitute in empty cavity wave equation results for “curl of curl”, simplify… (“s” and “q” are collected indices)
Multiply by conjugate then integrate:
Asq aq = l Bsq aq
Plug in expansion:
Start with wave equation:

## Slide 10: Computer implementation
Typical matrix size: 512, 2048, 8192 empty cavity eigenfunctions
Aitken method: extrapolate from 8192 to infinite number
“Singularity search method” to find eigenvalues rather than diagonalizing matrix
  Typical computation time: 0.5 hour if only TE (m=0), 2 hours if both TE and TM
  16 computing nodes, each with 12-core, 2.3 GHz Intel Haswell, 4 GB of memory

## Slide 11: Test vs. Theory
Infinite dielectric cylinder in infinite cavity
Match boundary conditions
Focus on one vertical section
Solve transcendental eqn numerically

## Slide 12: Modeling Stacked Dielectric Resonators

## Slide 13: Field patterns, two 3 mm DRs (er = 14)
Electric field
Magnetic field

## Slide 14: Comparison with Experiment
*extra empty cavity eigenfunctions needed

## Slide 15: Conclusions
Calculate resonant frequencies and field patterns, arbitrary arrangement of material (cylindrically symmetric)
  Error  0.4% for theory test (all but 1)
  Error  1.0% for experimental test (all but 1)
Issues: sharp features  more eigenfunctions needed, Gibbs phenomena in E
Download the code at http://www.physics.byu.edu/research/ coltonlab/cavityresonance
Contact me for preprint, john_colton@byu.edu

## Slide 16: Observing cavity resonances
The cavity resonance
Sweep microwave frequency, look for cavity absorption
Width  “Q factor”
  Q ~ 2000
Spin resonance experiment
“Park” at that microwave frequency
Sweep magnetic field to see spin response when hf = gmBB

## Slide 17: Summary of Technique
(but we don’t do it that way)

## Slide 18: Why not Faraday’s Law?
Instead…

## Slide 19: Computer implementation
What’s a “sound” method to index TE and TM modes with different radial and axial modes?
Let go from 1 to
Organized matrix size (typically size 512, 2048, 8192)

## Slide 20: Matrix diagonalization gets hard…
“Singularity search method”
Let be some small parameter
Scan
When is an eigenvalue, LHS should be zero, so will get really big to equal
Solve for the zeros of

## Slide 21: Aitken extrapolation
For a converging sequence
Define the sequence by the function , where the sequence converges to such that .
  Expand about …
Retain grid size, but increase number of eigenfunctions (6*20, 6*21, 6*22, ...)

## Slide 22: Electric field problems
Because we are solving for the displacement field D, E has some bad discontinuities

## Slide 23: Magnetic field
The magnetic field, on the other hand, is continuous everywhere (no magnetic material)
1st derivatives are problematic (discontinuous E)
We can smooth B and then differentiate to obtain smoothed E fields!

## Slide 24: Smoothed electric field
Polynomial fitting of order 3 over sections of 31 points (only across homogenous )

## Slide 25: Convergence issues
For small DRs, more eigenfunctions were needed to accurately represent the field
T-T 6 mm DRs
T-T 1.5 mm DRs

## Slide 26: Jaworski solution
Assumes and
Valid only for TE modes
Murata have and , accuracy of 1.0%
Trans-Tech have and varies from 0.15 to 0.6, accuracy of 12%