## Slide 1: Optically-measured electron spin lifetimes and spin relaxation in GaAs and SiC
EMN Meeting: Quantum Comm. & Quantum Imaging, Berlin, Aug 2016
John S. Colton
Physics Department
Brigham Young University, Provo, Utah
Student researchers:
Ken Clark Daniel Craft
Jane Cutler
David Meyer
Tyler Park
Phil White
Scott Crossen
Jacob Embley
Michael Meehan
Kyle Miller
Margaret Morris
Samples from
U.S. Naval Research Lab:
Allan Bracker
Sam Carter
Thanks also to (NRL):
Bradley Weaver
Evan Glaser

## Slide 2: Brigham Young University, Provo, Utah
Church sponsored (Church of Jesus-Christ of Latter-day Saints, Mormon)
30000 students (27000 undergrad, 3000 graduate)
70% of students speak a second language (many from church missions)
Physics: 30 faculty, 400 undergrads, 30 grads
  Consistently top 5 in U.S. for size & placement in physics grad schools

## Slide 3: Very Brief Outline
Introduction
GaAs
  Bulk
  Quantum wells
SiC vacancy defect
Conclusions

## Slide 4
Quantum computing via spin (1998)
http://www.research.ibm.com/ss_computing/
“DiVincenzo Criteria”
Scalable physical system with well-defined qubits
Preparable in |000...> state
Able to do many operations (~104) before decoherence
Universal set of gate operations
Accurate single qubit measurements
Optics!

## Slide 5: Time Resolved Faraday (or Kerr) Rotation (1998)
http://ime.uchicago.edu/awschalomlab/research/
Bulk GaAs
Awschalom group (UCSB, now Chicago)

## Slide 6: Optics to measure spin lifetimes
Initialize (polarize)
  Laser pump
  Thermal (low T, large B)
Depolarize
  Wait
  Microwave resonance
    Possibly repolarize via microwave pulses
Detect – laser probe
  Faraday/Kerr effect (rotation of linear polarization)
  Photolumimescence: degree of circular polarization
  PL intensity

## Slide 7: Time-resolved Faraday (Kerr) rotation
Initialize (polarize)
  Laser pump
  Thermal (low T, large B)
Depolarize
  Wait
  Microwave resonance
    Possibly repolarize via microwave pulses
Detect – laser probe
  Faraday/Kerr effect (rotation of linear polarization)
  Photoluminescence: degree of circular polarization
  PL intensity
Magnetic Field: parallel vs. transverse
(precession!)
Types of lifetimes: T1 vs. T2 vs. T2*

## Slide 8: Types of materials
Defects
  Donors in GaAs
  NV Center in diamond
  VSi in SiC
Quantum dots
  Gated QDs
  Self-assembled QDs
  GaAs QWs
Other?

## Slide 9: Importance of spin lifetimes
Materials characterization
Better understanding:
  Test existing theories
  Interesting new theories (e.g. Greilich et al., Mode locking in self-assembled QDs, 2006)

## Slide 10: T2* in Lightly Doped GaAs (2002)
Optical Orientation/PL Polar. Detection
Hanle Effect: Transverse Field  Lifetime from width
T2* = 26 ns
Phys Stat Sol (b) 233, 445 (2002)
n = 1E15 cm-3
T2* = 34 ns
Phys Solid State 39, 1765 (1997)
Phys Rev Lett 88, 256801 (2002)
Nominally undoped
T2* varies with Eexc
 changing n
 5 - 300 ns
Ioffe Institute

## Slide 11: Using Optics: III-V Semiconductors
Spin Orbit Coupling: J = L + S
CB
hh
lh
(Yu and Cardona)
so
Jz = 3/2
Jz = 1/2
L = 1
S = ½
 J = 3/2
-1/2
+1/2
-3/2
-1/2
+1/2
+3/2
-1/2
+1/2
L = 0
S = 1/2
 J = 1/2
Jz = 1/2
s+
Optical selection rules for circular polarized light
Spin Polarization ↔ Optical Polarization

## Slide 12: Measuring T1 (2003)
Why hadn’t it been done before?
  Too long!!
Idea:
Pulsed light

## Slide 13: Data: n = 110-15 cm-3 sample (2007)
Some raw data
T1 vs B for four temps
>20 ms (1.5K, 7T)
zoomed in
Beautiful exponential decays!
Theory: T1 decrease with B expected for QDs
1E15 sample

## Slide 14: Quantum-dot-like behavior?
Bulaev and Loss, PRB 71 205324 (2005)
Rashba spin relaxation
Our data

## Slide 15: Time-resolved Kerr rotation (cw lasers, modulated)
Solid State Comm. 152, 410 (2012)
GaAs substrate
AlGaAs barriers
2.8 nm well
4.2 nm well
6.2 nm well
8.4 nm well
14 nm well
n-GaAs Quantum Wells (2012)

## Slide 16: What do we expect?
Lack of bulk inversion symmetry  spin splitting of CB (“DP”)
D’yakonov and Kachorovskii (1986), QWs
Bastard & Ferreira (1992), ionized impurity
scattering
  ts = 2.5 ns for 15 nm well at 10 K
  perhaps 10-100 longer at 1.5 K
Bastard (1992), high fields (6-15 T)
  ts = 1-2 ns for 9 nm well, ~B1/2
Terauchi et al (1999), 300 K, DK verified in part
Lau (2001, 2002), 100+ K
  matched experiments of Terauchi, and Kikkawa & Awschalom
  also T2  T1
Various T2* measurements: a few ns in GaAs
  Longest lifetimes in any QWs: ~35 ns (II-VI)

## Slide 17: n-Doped QWs: Selection Rules
hh and lh degeneracy lifted
Singlet trion:
e + e + h(either  or , either hh or lh)
Kerr rotation:

## Slide 18: Wavelength Summary
Peak positions:
LH
HH

## Slide 19: Quantum Well Spin Decays!
ts = 85 ns
ts = 169 ns
pump and probe overlapped
5 K

## Slide 20: QW Spin Lifetimes, Summary
ts > 1000 ns!
Very long lifetimes!!
  Recall previous record was 35 ns (T2*)
Lifetimes increase with B
  But not B1/2 dependence

## Slide 21: Evidence of Two Spin Populations?
Localized vs. Delocalized
localized?
delocalized?
Compare: II-VI QWs
l1
l2
Zhukov et al, PRB 2007
(see also Hoffman et al, PRB 2006)
“LHT”

## Slide 22: Defects in SiC (2016)
Similar to diamond NV center
  Group IV: no nuclear spins
Potential advantages over NV
  Fabrication
  Cost
  Wavelengths (IR vs. visible)
Spin-dependent deep defect states
  Vsi
  Divacancies
  Antisite-vacancy pair
6H, 4H, and 3C polytypes
Irradiation: proton vs. electron
Riedel et al., PRL 109, 226402 (2012)
4H-SiC

## Slide 23: Silicon Vacancy Defects in SiC
  Divacancies
  20 K
  T2 times of ~1 ms
  Silicon vacancies
  Room temperature
  T2 times of ~160 µs

## Slide 24: Photoluminescence: Proton Irradiated Samples
6 K PL
Depth dependence

## Slide 25: Spin Dependence
Laser promotes electrons to higher energies
Non-radiative transition causes the ms=1/2 state to populate preferentially (and decreases photoluminescence)
Microwaves equalize spin populations, causing PL to increase

## Slide 26: ODMR
3/2  1/2 and
  -3/2  -1/2 peaks
Linear field dependence
10 GHz  0.358 T

## Slide 27: T2 via Optically-detected spin echo
Initialize (polarize)
  Laser pump
  Thermal (low T, large B)
Depolarize
  Wait
  Microwave resonance
    Possibly repolarize via microwave pulses
Detect – laser probe
  Faraday/Kerr effect (rotation of linear polarization)
  Photoluminescence: degree of circular polarization
  PL intensity

## Slide 28: Spin Echo
Submitted to Phys Rev B, 2016

## Slide 29: Spin Coherence vs. Temperature

## Slide 30: Similar Results Found by Others
Falk et al., Phys. Rev. Lett. 114, 247603 (2015)
  Measured T2* in silicon divacancies of 6H-SiC
Our results
Possible explanation: motional averaging from dynamic Jahn Teller effect. More theory needed!

## Slide 31: Conclusions
Optics for measuring spin lifetimes
Spin lifetimes for verifying and motiving theory
SiC as an interesting new candidate material
Funding acknowledgements
National Academies / NRC
Naval Research Lab
NSF
NASA
BYU
 If any of you are ever in Utah, please look me up!