## Slide 1: Ferritin-based semiconductor nanocrystals for solar energy harvesting
U of U seminar, Jan 13, 2016
Dr. John S. Colton
Physics Department, Brigham Young University
Undergrad students: Stephen Erickson, Cameron Olsen, Jacob Embley, Jake Maxfield, Alessandro Perego, et al.
Dr. Richard Watt
Ph.D. Student: Trevor Smith
Chemistry Department, Brigham Young University
Funding: Utah Office of Energy Dev., BYU Physics Dept, BYU Chemistry Dept

## Slide 2: Stereogram of ferritin
8 nm
8 nm

## Slide 3: Outline
Native ferritin: Fe(O)OH core
Optical bandgap measurements
Salts
Other metal(O)OH cores
Solar cell theory/efficiency calculations
A bit more synthesis: Mn and permanganate
Solar cell prototypes
The future

## Slide 4: Why is ferritin interesting?
Template for nanocrystals
  Ferroxidase center
Self healing against photocorrosion
Solubility
Photo-oxidation catalyst
1. Nanocrystal
From Watt, Petrucci, and Smith,
Catl. Sci. Technol. 2013

## Slide 5: Nanocrystals grown with ferritin
From Watt, Petrucci, and Smith, Catl. Sci. Technol. 2013

## Slide 6: Ferrihydrite basics
(Fe3+)2O3 • 0.5H2O
Nanomaterial
About 1100 Fe/ferritin
image: Wikipedia
Found in soils
Found in organisms
Similar to
hematite
Many defects
Lopez-Castro et al., Dalton Trans. 2012

## Slide 7: Examples of our samples
Non-native metal(O)OH samples
Take iron out: dithionite dialysis, 0.050 M TRIS-base buffer at pH 7.4 carefully titrated with NaNO3.
Putting iron (for example) back in: 10 mM ferrous ammonium sulfate added at a rate of 200 irons per ferritin every 10 minutes
Native
Manganese replacing iron

## Slide 8: Representative TEM images
unstained
stained with uranyl acetate
Use EDX to verify presence of substitutional elements in core
Use chemical techniques (Lowry, ICPMS) to establish # metal atoms/ferritin

## Slide 9: Nanocrystals grown with ferritin
From Watt, Petrucci, and Smith, Catl. Sci. Technol. 2013
1.0 – 3.5 eV

## Slide 10: Bandgaps via optical absorption
Xenon Arc Lamp
Spectrometer
Iris
Lens
Chopper
Sample (compare sample to blank)
Photodiode
Ref
Signal
Lock-in Amplifier
Computer steps through wavelength of spectrometer and records data from lock-in

## Slide 11: Typical Raw Data
With ferritin
Blank, solution with no ferritin

## Slide 12
Indirect gap
Direct transition
Defect State
Band gap
Higher
transition
Eg = 1.92 – 2.24 eV,
depending on size
direct = 2.92 – 3.12 eV,
depending on size
Ferrihydrite, Fe(O)OH

## Slide 13: Band structure of ferrihydrite in native ferritin
Figure from Colton et al, Nanotechnology (2014)
Compare table value: 2.5-3.5 eV
~1100 iron atoms per ferritin

## Slide 14: Band gap results
Size dependence:
quantum confinement
Anion dependence
(bonded to surface)
Figures from Colton et al, Nanotechnology (2014)

## Slide 15: Incorporating anions into the core
From Smith et al, J. Mater. Chem A (2015)
despite very small cores!

## Slide 16: Nanocrystals grown with ferritin
From Watt, Petrucci, and Smith, Catl. Sci. Technol. 2013

## Slide 17
Fe(O)OH
Fe
Fe
Nanocrystal synthesis: Fe-, Co-, Mn- and Ti(O)OH

## Slide 18
Metal3+(O)OH
Co2+ + H2O2
Fe2+ + O2
Mn2+ + O2
Nanocrystal synthesis: Fe-, Co-, Mn- and Ti(O)OH
(Cobalt with added peroxide)
Loading through ferroxidase centers
Notes: Iron(II) (for ferrihydrite mineral) and manganese (II) both use oxygen to load into ferritin. This is because the feroxidase center in ferritin (which is responsible for oxidizing metals) is able to oxidize the metal ions to a 3+ state. (Fe(II) Oxidation 0.77 V) Manganese has similar chemistry to Fe.
Cobalt is more difficult to oxidize (has a higher oxidation potential 1.7 V) and requires peroxide to increase the rate of cobalt loading into ferritin. (Peroxide -1.77 V)
Each metal oxide is unique, with its own photochemical and electrochemical properties.
18

## Slide 19: Substitutional metals
Co(O)OH
Mn(O)OH
Ti(O)OH
Eg
Direct transition
Total range: Eg from 1.60 – 2.29 eV
2.19-2.29 eV
1.60-1.65 eV
1.93-2.15 eV

## Slide 20: Multi-junction solar cells
Image from Wikipedia

## Slide 21: Efficiency calcs: Shockley-Queisser model
EF
EF
CB
VB
n-type
p-type
Photo-current
Recombination current
 depends on operating voltage
Arrows: direction of electrons

## Slide 22: Shockley-Queisser Results, 1961
Eg = 1.1 eV (silicon)  eff. = 29%
Best Eg = 1.34 eV  eff. = 33.7%, “SQ limit”
From Wikipedia, “Shockley–Queisser_limit”
(Using actual solar spectrum
rather than SQ’s 6000K
blackbody model of the sun)
Lose too much to phonons
Too much unabsorbed

## Slide 23: A Review of the Equations
Then compare Pmax to total solar energy
to define the efficiency
I
V
exponential with V
maximum
power
Blackbody spectrum
constant with V
concentration factor
Solar spectrum

## Slide 24: Multi-junction solar cells
Image from Wikipedia

## Slide 25: Extension to multiple layers, “i” = “ith layer”
Then compare Pmax to total solar energy to define the efficiency
Maximize P w.r.t. all of the Vi’s
(coupled nonlinear eqns, initialize by solving uncoupled case)
Not zero, because photons are absorbed by upper layers
Radiative recombination from layer just above
Radiative recombination from layer just below
Irecomb, i
(top layer: i=1)
General method of: De Vos, J Phys D (1980)

## Slide 26: Maximizing Power, Independent Cells
eff = 38%, w/o 1.1 eV layer
eff = 51%, with 1.1 eV layer
Black line: solar spectrum
Or PbS?

## Slide 27: Maximizing Power, Current Matched
eff = 42%, with 1.1 eV layer
Vtot = 5.5 V

## Slide 28
e-
Au
hv
Citrate
Citrateox
AuIII
Au0
e-
Metal oxide
core
Can we get the electrons out of the ferritin? Gold nanoparticle formation
Notes: Metal oxide reaction with light to form Au NP.
Note that the ferritin is colored based on the hydrophilic (blue) and hydrophobic (red) residues on the protein.
28

## Slide 29
Ti(O)OH and Gold Nanoparticles
Ti(O)OH
nanoparticle core
Protein
shell
Gold nanoparticles
attached to surface
20 nm
TEM image

## Slide 30
A little bit more synthesis: back to Mn
Eg goes down despite very small cores!

## Slide 31
Manganese with permanganate
 Also: permanganate only as a control (no iron, no Mn(II))
Notes: Figs: (a) Scheme using the reaction given in Eqn. 1. Mn(II) binds at the ferroxidase center (FC) and is oxidized to Mn(III) by permanganate. After oxidation the Mn(III) ions migrate to the ferritin interior and become mineralized as a Mn(III) compound such as Mn(O)OH. The Mn(V) is either recycled or disproportionates and forms MnO2. (b) Scheme for the reactions given in Eqs. 2 and 3. Manganese and permanganate first enter ferritin and then undergo a comproportionation reaction to form either a Mn(IV) or Mn(III) mineral.

## Slide 32
Manganese with permanganate
Most
permanganate
Results: success!
Least
permanganate
Mn(II):Mn(VII)

## Slide 33: Solar cell prototypes
Model: Dye sensitized solar cell (DSSC) / quantum dot solar cell
Electron flow
Electron flow to I-, (creating I3-)
Electron flow to QDs (changing
I3- to I-)

## Slide 34: QDSC band diagram
Image: Jordan Katz
https://www.ocf.berkeley.edu/~jordank/Jordan_Katz/Research.html
Notes: 34

## Slide 35: Fabrication
TiO2 preparation and deposition
Ferritin deposition
Counter electrode preparation
Assembling the cell and electrolyte injection

## Slide 36: First Results
Open circuit voltage measurements of the different DSSCs fabricated.
Ferritin-Mn open circuit voltage measurement

## Slide 37
I-V curves
Native ferritin
Issues: consistency, cracking, absorption, ferritin-TiO2 transfer
Plans: pre-made cells, solar filter, genetically altered ferritin?
Optimal conditions
(but efficiency low)

## Slide 38: Conclusions
We’ve now got a large variety of ferritin-based nanoparticles
Multiple band gaps  Large theoretical efficiencies
Maybe we can make an efficient solar cell
Future work:
  More solar cell prototypes
  PbS nanocrystals
  Platinum nanoparticles?  Hydrogen gas
  Ferritin particles as catalysts, esp. reducing oxygen in fuel cells
Refs:
Colton et al., Nanotechn 25, 135703 (2014)
Smith et al., J Mater Chem A 2, 20782 (2014)
Erickson et al., Nanotechn 26, 015703 (2015)
Olsen et al., to be submitted soon
Perego et al., still in progress