## Slide 1: Oxidation-Reduction Potential of Iron Encapsulated by Ferritin
Jacob Embley
Dr. John Colton, Dr. Richard Watt, Trevor Smith, Cameron Olsen, Kevin Zenner, and Stephen Erickson
Notes: Introduce yourself

## Slide 2: What is ferritin?
Spherical protein complex
Nano-cage composed of 24 sub-units
Approximately 12 nm in diameter
Intracellular complex found in nearly all organisms
Organisms use ferritin to store and regulate iron

## Slide 3: Ferritin further explained
Hollow 8 nm diameter interior
Natively encapsulates ferrihydrite nanoparticle
Up to 4500 Fe atoms per ferritin
Ions enter through 3-fold channels
Notes: Shorten these bullets

## Slide 4: Why is ferritin interesting?
Photovoltaic device
Nanobattery

## Slide 5: Batteries
Two half-cells
Current flows across the potential difference
Reduction and oxidation occur at the electrodes
Common issue:
  Battery performance deteriorates after repeated charge and discharge cycles

## Slide 6: Potential use of ferritin in a battery
Electrodes composed of Ferritin cores of varying reduction potentials
Advantage of this type of battery:
  Ferritin protects and maintains the metal core

## Slide 7: Effects of salt anions on reduction potential
Notes: Enlarge the graphic

## Slide 8: Determining the Reduction Potential
Potentiostatic coulometry
Cyclic Voltammetry

## Slide 9: Potentiostatic coulometry
Time
Current
Notes: Try to show some real data

## Slide 10: Results from potentiostatic coulometry

## Slide 11: Cyclic voltammetry
Cl-
Br-

## Slide 12: Results from cyclic voltammetry

## Slide 13: Ongoing and Future studies
Testing the battery performance of the ferritin cores:
  Rate of charge and discharge
  Life cycle tests
Reduction Potential of non-iron metal oxide cores in Ferritin

## Slide 14: Conclusion
The reduction potential of the iron mineral nanoparticle encapsulated by ferritin is significantly altered by the addition of various salt anions
Anion | Coulometery Reduction | CV Reduction (mV) | CV Oxidation (mV)
Cl- | 500.7 ± 8.35 | 108 ± 52 | 286 ± 40
Br- | 436.3 ± 10.8 | -74.0 ± 31 | 110 ± 26
VO33- | --- | 353 ± 74 | 476 ± 80
PO43- | 463.5 ± 12.4 | 133 ± 35 | 285 ± 19
MoO42- | 445.6 ± 11.8 | 42.0 ± 52 | 240 ± 22
WO42- | 411.0 ± 12.4 | 73.0 ± 61 | 291 ± 31