## Slide 1: Temperature and sample dependence of spin echo in SiC
Kyle Miller, John Colton,
Samuel Carter (Naval Research Lab)
Brigham Young University Physics Department
NSF Grant PHY1157078

## Slide 2: Background: Defects in SiC
The goal is to use silicon carbide defects for quantum information purposes (qubits)
  SiC is cheaper than diamond and can be grown on a lattice
Defects occur where a silicon atom is missing
Determine spin coherence time of electrons in defects
From Riedel et al., Phys. Rev. Lett. 109, 226402 (2012)
From Florian et al., “Advances in Ceramics - Synthesis and Characterization, Processing and Specific Applications“ (2011)

## Slide 3: Background: Electron spins and ODMR
Laser promotes electrons to higher energies
Non-radiative transition causes the ms=1/2 state to populate faster
Microwaves equalize spin populations, causing a decrease in the observed photoluminescence (PL)
4A
4E
1/2
3/2
1/2
3/2
Metastable
doublet
See P. G. Baranov et al., Phys. Rev. B 83, 125203 (2011)
optical
Non-radiative
2D
B
ms=+3/2
ms=-3/2
ms=+1/2
ms=-1/2
4H-SiC, S=3/2 system
Energy
From Sam Carter

## Slide 4: Experimental Setup
Coupling loop is made from the inner conductor of the coax
Sample placed directly on the copper cold finger
B0
Bµwave
SiC
Laser
Towards table
(schematic rotated from photo)

## Slide 5: ODMR
Two resonant peaks, one varies in strength
Linear field dependence
Very close to 2

## Slide 6: % ODMR
Measure of the percent change in the PL when at resonance
Better SNR with lower temperature because of larger % ODMR.

## Slide 7: Rabi oscillations
These occur when electrons are continuously switched between spin states (See video)
Stronger microwave power means faster oscillations
This gives and pulses (which flip spins upside down and half-way upside down)
Laser
Laser
Vary length
(0 – 1000 ns)
1 µs
5 µs
207 MHz
250 MHz

## Slide 8: Spin echo
Laser
Laser
2 µs
20 µs
Set , then vary to observe the signal
Microwave pulses manipulate spin orientation
Signal is seen when pulses are equally spaced
"HahnEcho GWM" by GavinMorley - Gavin W Morley. Licensed under Creative Commons Attribution-Share Alike 3.0 via Wikimedia Commons - http://commons.wikimedia.org/wiki/File:HahnEcho_GWM.gif#mediaviewer/File:HahnEcho_GWM.gif
See video

## Slide 9: Spin echo data
Exponential decay of the signal predicts
All further data obtained with B0 ≈ 350 mT, f0 ≈ 10.5 GHz

## Slide 10: Calculating T2
Fitting the exponential decay of the spin echo signal gives T2

## Slide 11: Summary of T2 Lifetimes
Lifetime appears to be independent of temperature, decreases with defect concentration
Samples with fewer defects have less PL (more noise), need more testing
Less noise at lower temps

## Slide 12: Defect Concentration
Nature of photoluminescence (PL) varies with temperature, defect concentration and type

## Slide 13: Electron-irradiated sample
Spin echo signal does not decay within our available measurement time
Lower bound of τ > 40 µs

## Slide 14: Summary
Spin coherence time
  1013 cm-2 proton-irradiated ≈ 64 µs (6 K)
  1014 cm-2 proton-irradiated ≈ 16 µs (5-296 K)
  1017 cm-2 electron-irradiated > 40 µs (296 K)
Is this long?
  Typical lifetimes are 10-100 µs for SiC
Can we get longer?
  Maybe with defect concentration and/or type
  What is the limiting factor on the lifetime?
Future work
Try electron-irradiated samples with varying defect concentrations

## Slide 15: Experimental Setup
Temperature = 5 – 296 K
B0 up to 1.36 T
Microwaves at 25 W
870-nm laser at 0.7 W
µwave
source
Cryostat
Electro-
magnet
B0
Bµwave
SiC
Laser

## Slide 16: Maximizing microwave power
Stub tuners, or “slide trombones”, help tune standing wave patterns
They match the impedance of the loop for maximum radiation output
Double stub
Single stub

## Slide 17: ODMR – Microwave power
Increased response with increased microwave power
Width also increases