## Slide 1: Electron Spin Coherence of Silicon Vacancies in Proton-Irradiated 4H-SiC
APS March Meeting, Mar 14, 2017
John S. Colton
Physics Department
Brigham Young University
Co-authors:
J. S. Embley,* K. G. Miller, M. A. Morris,* M. Meehan, S. L. Crossen
Students at BYU
*funded by NSF RUI program (M.A. Morris visiting from Brandeis U)
B. D. Weaver, E. R. Glaser, and S. G. Carter
Naval Research Lab
Helpful discussion: Michel Bockstedte, University of Salzburg
Embley et al., PRB 95, 045206 (2017)

## Slide 2: Motivation: long T2 coherence times
NV center in diamond
  3 ms at 300 K, 600 ms at 77K (Bar-Gill, Nat Comm 4, 1743, 2013)
  Many, many others
4H SiC divacancies:
  360 us at 20 K, 50 us at 300 K (Falk, Nat Comm 4, 1819, 2013)
  184 us at 20 K, 263 us at 200 K (Koehl, Nat 479, 84, 2011)
  1.2 ms at 29 K (Christle, Nat Mater 15, 160, 2015)
4H Vsi
  81 us at 300 K (Carter PRB 92, 161202, 2015)
  160 us at 300 K (Widmann Nat Mat 14, 164, 2015)
Can likely be extended via dynamical decoupling pulse sequences such as Carr-Purcell-Meiboom-Gill (CPMG)

## Slide 3: How does T2 change with temperature?
?
T1 vs. temperature for Vsi
Phonon effects  monotonic decrease with temperature
Simin et al, arXiv:1602.05775v1 (2016)

## Slide 4: Another motivation: proton irradiation
Plotting the vacancy-related PL
1012 cm-2 sample
diffuse
region
concentrated
region

## Slide 5: SiC samples
Proton irradiated 4H SiC
  2 MeV protons, fluences of 1011,1012,1013, and 1014 cm−2
Single vacancy electronic defect states, most at ~34 um below surface
  Defect concentrations  3  1011, 3  1012, 3  1013, 3  1014 cm-3 in diffuse regions, ×10 in stopping layer
1012 cm-2 sample

## Slide 6: Optically-detected magnetic resonance
Spin 3/2 system
Polarized via optical pumping
Detected via change in PL
(turned 90)
Laser hits sample edge on

## Slide 7
10.49 GHz transition

## Slide 8: Spin Echo

## Slide 9: Biexponential vs. Stretched Exponential
Assumes two populations
However, long time component has more amplitude than short time component (opposite to expected)
Distribution of lifetimes
Has been used in SiC phenomenologically with b = 2 (compressed) (Christle, 2015)
Our fits b = 0.5-0.8
  mean T2 times of 1.3-3.3 t
  widths of 2.5-14 t
Wikipedia
1012 cm-2 sample

## Slide 10: Coherence times vs. temperature
A. L. Falk et al. PRL 114, 247603 (2015).
tlong
Longer times
Shorter times

## Slide 11: Motional/dynamic Jahn-Teller effect
Thermally activated rapid reorientation of the vacancy (bond switching)
Example: Positively charged VC in SiC, Umeda PRB 70, 235212 (2004)
Above 40 K, linewidth narrows with temperature (T2 increases)

## Slide 12: Conclusions
T2 coherence times up to 270 us (8 K, lower doped sample)
  Dipole-dipole interactions are significant
Motional Jahn-Teller effect lengthens times from ~60-150 K
Inhomogeneous distribution of spins
Embley et al., PRB 95, 045206 (2017)

## Slide 13: 1013 cm-2 sample results

## Slide 14: 10-14 cm-2 sample results

## Slide 15
Spatial/spectral map of V1 vacancies along a line
In 1e11 cm^-2 proton irradiated epilayer
Jumps/gaps in ZPL should indicate individual Si vacancies
Estimate on the order of 1 vacancy per mm
Depth resolution roughly 2-3 mm
Assume V1 and V2 about the same density (pretty good assumption)
Position (mm)
Emission energy (meV)
V1
0
6
12
18
24
30
1436
1438
1440
1442
This was taken at a position well above the higher density region at the stopping range of protons
About 0.3/mm^3 = 3e11cm^-3 for proton irradiation at 1e11cm^-2
For 1e13cm^-2 irradiation, assume 100 times higher density
This is the density above the proton end of range at about 32um. At the
Stopping range that density is about 20 times higher.