## Slide 1: Measurement of Spin Coherence Times in Proton-Irradiated 4H-SiC
Jacob Embley
Research Advisor:
Dr. John Colton
Collaborators:
Dr. Sam Carter (Naval Research Lab)
Margaret Morris
Kyle Miller
Michael Meehan
Funding:
National Science Foundation,
Grant PHY-1461219
BYU Physics Department

## Slide 2: Silicon Vacancy Defects in SiC
  Divacancies
  20 K
  T2 times of ~1 ms
  Single vacancies
  Room temperature
  T2 times of ~160 µs

## Slide 3: Silicon Carbide Samples
4H-Silicon Carbide (SiC)
Single vacancies
  1013 and 1014 cm-2 proton-irradiated (2 MeV)
ODMR and Spin Echo

## Slide 4: Energy Levels
1/2
3/2
1/2
3/2
See P. G. Baranov et al., Phys. Rev. B 83, 125203 (2011)
optical
Non-radiative
2D
B
ms=+3/2
ms=-3/2
ms=+1/2
ms=-1/2
S=3/2 system
Energy

## Slide 5: Rabi Oscillations

## Slide 6: Spin Echo

## Slide 7: Spin Echo Decay
T2 = 163.7 µs
T2 = 50.6 us
T2
T2

## Slide 8: Spin Coherence vs. Temperature

## Slide 9: Similar Results Found by Others
Falk et al., Phys. Rev. Lett. 114, 247603 (2015)
  Measured T2* in silicon divacancies of 6H-SiC
Our results

## Slide 10: Conclusions
Highest temperatures limit spin coherence
Longer coherence times for less-irradiated sample
Future work:
  Explain the temperature dependence

## Slide 11: Experimental Set-up