## Slide 1: Lead Sulfide Quantum Dot Band Gap Investigations
J. Ryan Peterson
Thanks to:
Dr. John S. Colton (advisor)
Kameron Hansen, Luis Perez, Cameron Olsen

## Slide 2: Quantum Dot Synthesis
Different core sizes
Notes: Explain how image was taken
Explain PL briefly
Mark FWHM and write that it equals .3eV explicitly

## Slide 3: Band gap distribution
FWHM: 0.3 eV
FWHM: 0.007 eV
Notes: Show a plot of a sharp PL result due to a single narrow band gap
Mark FWHM, write the number (.005eV or whatever)
Explain that the PL spectrum would be even narrower but is limited by the spectrometer resolution

## Slide 4: Varying Band Gap Energy Using the Brus Equation
PbS quantum dot band gap
Bulk PbS band gap
Notes: Show plot for Brus predictions on this page
Explain quantum confinement in the nanoparticles; that is why the band gap increases as the radius decreases.
If I have time, an even more thorough explanation might be good.
Explain how it was derived (assuming parabolic band structure and assuming periodic wavefunctions, so no edge effects)

## Slide 5: Photoluminescence Experimental Setup
398nm Diode Laser
Sample
0.25m Spectrometer and Germanium Detector
Notes: Label setup: sample, laser, spec, etc.
Say short wavelength, not high energy (they might think high power)

## Slide 6: PbS Photoluminescence
Signal adjusted for system sensitivity
Measured signal
Half max
Signal adjusted for system sensitivity
Measured signal
Half max
Notes: Explain how the orange line is calculated

## Slide 7: Size and Band Gap Results
Sample | Measured Radius | Expected Band Gap (Brus equation) | Measured Band Gap and FWHM
Sample 1 | 2.25 ± 0.48 nm | 1.70 eV (1.29 eV - 2.50 eV) | 1.33 eV (0.33 eV)
Sample 2 | 3.03 ± 0.39 nm | 1.12 eV (.97 eV – 1.35 eV) | 1.14 eV (0.31 eV)
Sample 3 | 3.04 ± 0.54 nm | 1.12 eV (.92 eV – 1.46 eV) | 1.23 eV (0.23 eV)
Sample 4 | 5.70 ± 0.89 nm | 0.61 eV (.56 eV - .69 eV) | 1.0 eV (0.3 eV)
Sample 5 | 6.10 ± 0.89 nm | 0.59 eV (.54 eV - .65 eV) | < 1.0 eV
Notes: Explain why we couldn’t measure below 0.93 eV
Explain that when the radius gets small, the assumptions made by the equation don’t hold. It assumes periodic wavefunctions, but the wavefunctions become very nonperiodic when
Aerobic Sample 1
Aerobic Sample 3
Anaerobic Sample 3
Anaerobic Sample 6
Aerobic Sample 6

## Slide 8: Protection Against Photocorrosion
Fe(III) oxide Fe2+ (aq.) Fe3+ (aq.) Fe(OH)3
Catalysis Science & Technology, 2013, 3, 3103
Notes: Cite ref in small print, may abbreviate
Find a different figure that is simpler or explain better what is going on in it.
Look up this equation again in Richard’s paper

## Slide 9: Thioglycerol PbS Time-Dependent PL
Spectra taken at 5 minute intervals
Notes: This data was taken every four minutes, with the direction of the intensity and band gap indicated by the blue line.
Ask for advice on legend
Mention that after 3 hours, the emission was only 31% of the peak
Try rainbow plot colors
Write the illumination intensity and time interval on graph

## Slide 10: Ferritin PbS Time-Dependent PL
Notes: PL Amplitude only decreases to 61% of original by 3 hours. By 10 hours, still 59%.
Explain why it is so noisy (weaker signal)
Maybe repeat to get clearer data

## Slide 11: Thioglycerol PbS Photocorrosion
Thioglycerol-capped PbS
Before
After
Ferritin-enclosed PbS
Notes: Explain what these samples were exposed to: Xenon arc lamp at 3x solar intensity for two hours

## Slide 12: Conclusions and Future Work
Ferritin core size and band gap widely tunable
Ferritin effectively protects against photocorrosion
Thio-PbS 3 hours
FTN-PbS 3 hours
Notes: Explain that these samples

## Slide 13: Measurement limits
Signal adjusted for system sensitivity
Measured signal
Half max
Detector Response
Notes: Explain spec response too

## Slide 14: Ferritin PbS Time-Dependent PL
1.2 eV
Notes: Point out stable band gap
This graph could be optional (or maybe both this and previous graph on one slide)

## Slide 15: Thioglycerol PbS Photocorrosion
Thioglycerol-capped PbS
Ferritin-enclosed PbS
Notes: Explain what a capping agent is again
Explain what these samples were exposed to: 400nm laser, 100mW, unfocused
Explain what area the laser hit
Maybe don’t include this slide