## Slide 1: Time-Correlated Single Photon Counting (TCSPC)
Scott Thalman
Brigham Young University
Advisor: Dr. John Colton
Dr Haeyeon Yang USU Physics
Help from Mitch Jones, Steve Brown, Dallas Smith
Notes: Add other names, plan to do not have done, also use tcspc, haeyeon and matt asplund, add BYU, introduce myself

## Slide 2: Overview
Time-correlated single photon counting (TCSPC) measures photoluminescence (PL) lifetimes
  Pulsed laser illumination source
  Single-photon detectors
  Very fast timing module
100 picosecond time resolution with deconvolution
InGaAs Quantum Dots
Optical properties are an indicator of sample quality
Notes: Spell out tcspc

## Slide 3: Photoluminescence
e
-
e
-
e
-
Excitation
Relaxation
Ground State
(valence band)
Excited States
(conduction band)
Photon
Energy Gap
e
-
Notes: Ground state equivalent, maybe add a slide after with a PL scan

## Slide 4: Quantum Dots
GaAs
Scanning tunneling micrograph of InGaAs Quantum Dots on GaAs substrate
Dong Jun Kim et al 2008 Nanotechnology 19 47560
GaAs
QD
40 nm
InGaAs
Notes: Thin out wetting layer, add scale,

## Slide 5: Quantum Dots
Confined electrons must occupy energy states that fulfill the Schroedinger equation
  Results:
  Discrete energy levels
  Discrete luminescence wavelengths
http://www.vectorsite.net/tpqm_02.html
Energy
Notes: Compare to infinite square well

## Slide 6: QD Photoluminescence

## Slide 7: Time Correlated Single Photon Counting
QD
Sample
Pulsed Laser
~30 fs, center wavelength 800 nm
Si-APD
Detector
Fast
Photodiode Detector
Ortec Fast Digitizer
Timing Module
Start
Stop
Lenses and Filters
Notes: Bigger

## Slide 8: QD Fluorescence Lifetime Expected Results
Mazur et al 2006 Journal Of Applied Physics 100 054313
Fluorescence lifetime of InGaAs Quantum Dot (fig 1) and Quantum Well (fig 2) samples measured by a streak camera.
Fig 2
Fig 1
Notes: Image of haeyons qd chains, islifetime different from chains to dots, CdSe dots,This is not our data, don’t mention streak camera

## Slide 9: InGaAs QD Results
Instrument Response
Notes: Present the convolution as a problem and our solution.

## Slide 10: InGaAs QD Results: Convolution
Definition of Convolution
Convolution Theorem
Notes: Add slide with summary of results. Make curves thicker, get rid of reconvolution

## Slide 11: Summary of Results
Sample Number | Photoluminescent Lifetime (ns) | 
 | Unfocused Laser | Focused Laser
032607-A | 0.86 | 0.65
032607-B | 0.78 | 0.78
032907 | 0.96 | 0.60

## Slide 12: Conclusion
Using TCSPC we were able to measure the photoluminescent lifetimes of self-assembled InGas QDs to help determine their quality.
Our samples had lifetimes of 0.6-1.0 ns.
Using deconvolution we were able to enhance our results.
Future studies will determine if quantum structures such as QD chains can be formed by this growth method.
Thank You