## Slide 1: Properties of protein-based ferrihydrite nanoparticles
Stephen Erickson
Trevor Smith
Dr. John Colton
Dr. Richard Watt
Special thanks to the NSF for funding
Ferritin
Ferrihydrite

## Slide 2: Motivation
Previous studies do not agree on the band gap, giving values from 1.1-3.5 eV
Self assembling cores, allows for controlled size and composition
Seek to show tunable band gaps
  Useful for light harvesting, detectors, etc
Provide experimental evidence for hypothesized aging effect

## Slide 3: Direct and indirect band gaps
Indirect band gaps require a phonon to be emitted or
absorbed in order to conserve momentum.
Images courtesy of Wikipedia

## Slide 4: Experimental setup
Xenon Arc Lamp
Spectrometer
Iris
Lenses
Chopper
Sample Holder
Photodiode
Ref
Signal
Lock-in Amplifier
Computer steps through wavelength of spectrometer and records data from lock-in

## Slide 5: Typical raw data
Control
With ferritin

## Slide 6: Data analysis
direct gap
indirect gap, phonon emitted
We arrive at the band gap by plotting α2 and α1/2 versus
phonon energy then extrapolating a linear fit to the x-axis
Absorption coefficient α:

## Slide 7: Extrapolating band gaps
Indirect gap
Direct transition

## Slide 8: Possible band structure

## Slide 9: Different core sizes
Smaller particle
→ larger gap
Core crystallizes
with time
1500 Fe atoms
1000 Fe atoms
500 Fe atoms
Image courtesy
http://hyperphysics.phy-astr.gsu.edu/hbase/quantum/imgqua/pbox1.gif

## Slide 10: Different core sizes – direct transition
1500 Fe atoms
1000 Fe atoms
500 Fe atoms

## Slide 11: Summary
Reconciled previous band gap studies
Showed tunable band gaps through different particle sizes
Provided first experimental evidence of theorized aging effect
Future experiments will focus on demonstrating even greater control over the band gap through different mineral cores, like Co, Mn, Ni, etc.