## Slide 1
Tunable band gaps of protein enclosed nanocrystals for high efficiency solar energy conversion
Stephen Erickson
Trevor Smith
Dr. Richard Watt
Dr. John Colton
APS Four Corners Meeting
October 17, 2014

## Slide 2: Ferritin protein
Template for controlled, uniform, and self-assembling nanocrystal synthesis
Ferroxidase center captures loose metal ions and reattaches them to the nanocrystal
Can be deposited in ordered arrays on a substrate

## Slide 3
Matsui, et al Jpn. J. Appl. Phys., 46, L713-15

## Slide 4: Motivation
Single junction photovoltaic cells are subject to the Shockley-Quieisser limit of 33.7% efficiency.
Layered PV cells of multiple band gaps have reached efficiencies of 44%.

## Slide 5: Experimental Methods
Control
With ferritin
Blank, solution with no ferritin
Optical absorption spectroscopy:
  Transmitted power through the sample is compared to a control to get percent transmitted as a function of wavelength
  After some mathematical analysis, linear fits are extrapolated to the x-axis to find the band gap
For a more detailed description, see: J.S. Colton, S.D. Erickson, T.J. Smith, and R.K. Watt, Nanotechnology 25 135703 (2014)

## Slide 6: Co, Mn, and Ti-oxides

## Slide 7: Co-depositing anions into Fe(O)OH

## Slide 8
520 nm
775 nm

## Slide 9: Calculating theoretical efficiencies
Use a detailed balance model similar to Shockley and Queisser
Coupling between the layers due to mutual irradiance
Maximizing the electrical power yields a system of coupled transcendental equations:

## Slide 10: Solving the system of equations
Solving for optimal operating voltages must be done numerically, which requires a good initial guess to converge on the solution
Ignoring coupling between layers, each can be optimized independently from a single transcendental equation:

## Slide 11: Maximum Efficiency
AM 1.5G spectrum
I-V Characterisitics

## Slide 12: Current Matching
Advantage:
  Higher output voltage
Disadvantage:
  Current limited by lowest producing cell

## Slide 13: Efficiency Table
 | fW (# suns) | Operating voltages (V) | Theoretical efficiency (%)
Ti,Fe,Co,Mn | 1 | 1.856,1.680,1.490,1.181 | 38.0
 | 100 | 1.974,1.798,1.607,1.298 | 41.0
 | Max | 2.130,1.954,1.764,1.453 | 44.9
Ti,Fe,Co,Mn,Si | 1 | 1.856,1.680,1.490,1.191,0.748 | 51.3
 | 100 | 1.974,1.798,1.608,1.308,0.864 | 56.4
 | Max | 2.130,1.954,1.764,1.464,1.012 | 63.1
Ti,Co, Mn,Si | 1 | 1.905,1.505,1.251,0.825 (5.49 total) | 41.6
(current matched) | 100 | 2.024,1.622,1.370,0.944 (5.96 total) | 45.2
 | Max | 2.182,1.778,1.527,1.103 (6.59 total) | 50.0

## Slide 14: Conclusions
Band gaps of ferritin enclosed nanocrystals can be tuned to cover most of the visible spectrum, from about 520-775 nm
These materials show promise in solar energy applications, with high potential efficiencies
Future work will characterize II-VI semiconductors
For more information see: TJ Smith, SD Erickson, CM Orozco, A Fluckiger, LM Moses, JS Colton, and RK Watt, submitted to J. Mater. Chem. A. (2014) SD Erickson, TJ Smith, LM Moses, RK Watt, and JS Colton, submitted to Nanotechnology (2014)