## Slide 1: Characterization of quantum dot chains using transmission electron microscopy
Tyler Park
Jeffrey Farrer
John Colton
Haeyeon Yang
* Special thanks Felipe Rivera and Thomas McConkie for sample preparation (FIB/SEM)
APS March Meeting 2012, Boston

## Slide 2: Introduction
Dong Jun Kim and Haeyon Yang,
Nanotechnology,(2008).
Zh. M. Wang, et al.,
Journal of Applied Physics, (2006).
What are quantum dot “chains?”
What is their significance?
  Optoelectronic Devices
  Conduit for spin information W. V. Schoenfeld et al., Appl. Phys. Lett. (1999)
(110)

## Slide 3: Previous work
Prepatterned Substrates Lee et al., Nanotechnology, (2006)
Stranski-Krastanov (1939)
InGaAs
Strain driven self-assembly M. Riotte et al., Applied Physics Letters, (2004)

## Slide 4: Our samples
Grown at lower temperature so quantum dots don’t form yet
Annealing process, during which dots are formed
  More control on growth A.O. Kosogov et al., Appl. Phys. Lett. (1996)
3 samples with slightly different growth parameters
InGaAs

## Slide 5: Our Samples - methods
Photoluminescence (PL) spectroscopy
Time-resolved PL
Transmission electron
microscopy (TEM)
  Chains with GaAs cap*
  Chemical analysis
    Partial electron energy-loss spectroscopy (PEELS)
    X-ray energy dispersive spectroscopy (XEDS)
*Zh. M. Wang et al., Journ. Of App. Phys. (2006)

## Slide 6: Sample preparation
Focused Ion Beam (FIB)
Cross-section cuts
  Lift-out method
Plan view cuts
  Our own method?

## Slide 7: Issues
Contamination
  Damage from silicon sample holder
Cross-section cuts
  Difficult to see an individual dot
Plan view cuts
  Quantum dots are close to surface
  Thinning issues
  Platinum deposits

## Slide 8: Current results
032607B
032607B
032607A
Images
Chemical Analysis:
  032607B (EDS)
GaAs cap
InGaAs layer
GaAs bulk
GaAs cap
InGaAs layer
GaAs bulk

## Slide 9: summary
The quantum dots seen, but not individually
Chemical analysis is so far close to what we were expecting
Continue with chemical analysis on cross-section cuts
Find a practical way of obtaining a plan view cut
Future work: Spin information transmission?