## Slide 1: Characterizing epitaxially-grown InGaAs quantum dot chains using transmission electron microscopy
Tyler Park
John Colton Haeyeon Yang*
Jeff Farrer
APS March Meeting 2013 Baltimore, MD
* South Dakota School of Mines

## Slide 2: Outline
Quantum dots – Growth
Quantum dot chains
Motivation
Transmission Electron Microscopy (TEM)
Results

## Slide 3: Quantum Dot Growth
Self-Assembled
Modified Stranski-Krastanov Method
  Wetting layer grown at cooler temperature
  Annealing process added
GaAs Substrate
GaAs
GaAs
InGaAs

## Slide 4: Quantum Dot Chains
STM Images (Uncapped samples)
  Wetting layer thickness affects QD shape
Kim & Yang, Nanotech 19, 475601 (2008)
(110)
(110)

## Slide 5: Quantum Dot Chains
Yang accomplished forming QD chains on a non-patterned substrate
Dong Jun Kim and Haeyon Yang,
Nanotechnology,(2008).
Zh. M. Wang, et al.,
Journal of Applied Physics, (2006).
T. V. Hakkarainen et al. Journal of Appl. Phys., (2011).

## Slide 6: Motivation
Tunable in infrared wavelengths
Applications:
  Optoelectronics
  Infrared Detectors/Lasers (Fujitsu and Tokyo University (2010), P. Martyniuk and A. Rogalski. (2008))
  Quantum Computing (Albert M. Chang. (2001))
Capping layer known to alter nature of dots (D. Awschalom et al. (2002))
Physical measurements

## Slide 7: Transmission Electron Microscopy
Sample
Electron source
Apertures
Electromagnetic Lenses

## Slide 8: Transmission Electron Microscopy
Sample
Electron source
Apertures
Electromagnetic Lenses
e-beam
direct beam
diffracted beam

## Slide 9: Transmission Electron Microscopy
Two-Beam condition
  Diffraction contrast – strain contrast
220
220
220
000
400
000
220

## Slide 10: Transmission Electron Microscopy
Cross-sectional and plan view cuts
  Annealing temp.: 460°C, 480°C, 500°C
Analytical transmission electron microscopy (chemical analysis)
  Parallel electron energy-loss spectroscopy (PEELS)
  X-ray energy dispersive spectroscopy (XEDS)

## Slide 11: Sample Preparation
Cross-section Cuts
  Focus Ion Beam (FIB) – Lift-out method
Plan View Cuts
  Lift-out method
  Hybrid method
    Mechanical thinning
    FIB
FIB
Mechanically thinned sample
QD layer

## Slide 12: Results
Cross-section Images
  2-beam conditions
    Diffraction contrast (Strains)
  STEM
  Mass Thickness Contrast
  HRTEM
Measurements
  Current task, incomplete results
  Show that dots flatten w/ annealing temperature
Chemical Analysis:
  ~10% Indium in the 500°C sample
  ~2% Indium in the 460°C sample (redo)
  ~5% Silicon contaminates!
GaAs Cap
GaAs
InGaAs QD layer
460°C
480°C
500°C
~15 nm
~10 nm
In Progress

## Slide 13: Results
Plan View Images
  2-beam conditions
    Diffraction contrast (Strains)
Measurements
  Separation of chains/dots
  Dot dimensions
500°C
~90 nm
~30nm

## Slide 14: Conclusions
Dots have formed as expected
  Capping layer has little effect
  Chains in all 3 samples
Measurements (height x width x chain separation):
  460°C: 15nm x 30nm x 70nm
  480°C: ??nm x 35nm x 90nm
  500°C: 10nm x 30nm x 90nm
Chemical Composition
  Estimated to be 10% In, 35% Ga, 50% As, 5% Si (from the sample annealed at 500°C)
Special thanks to Felipe Rivera and Thomas McConkie for assistance w/ lift-out